## Slide 1
Advanced petrology: kinetic theory in petrology
Course: 650.810
7-lecture: Point defects and diffusion, Mineral nucleation and growth

## Slide 2
Yakov Frenkel (or, sometimes, Jakov or Jacov) proposed
in 1926 and then elaborated the idea of diffusion in
crystals through local defects (vacancies and interstitial
atoms). He introduced several mechanisms of diffusion
and found rate constants from experimental data. Later,
Nowadays, it is universally recognized that atomic defects
are necessary to mediate diffusion in crystals

## Slide 3
Crystal defects
Point defects: Defects in the periodic structure of a crystal caused by the absence of an atom
or ion at a lattice site (vacancy), the presence of an additional atom in an interstitial position,
or the presence of a foreign ion at a lattice site (impurity)
The periodic crystal structure of solid crystal can be defected by four types of defect.
Point defects
Line defects
Planar defects
Bulk defects

## Slide 4
Crystal defects
Taking into account the restriction of electroneutrality. When an ion is removed from a lattice
Site, the crystal acuires a charge imbalance. This imbalance must be corrected if
Electroneutrality is to be mantained. In a simple ionic crystal there are two dominant types of
intrinisc defects
1- Schottky defect
Anti-Schottky defect
2- Frenkel defect
Anti-Frenkel defect
Point defects

## Slide 5
Crystal defects
Line defects: are linear defects around which some of the atoms of the crystal lattice are
misaligned.
There are two basic types of line defects, the edge defect and the screw defect.
"Mixed" defects, combining aspects of both types, are also common.
Edge defects are caused by the termination of a plane of atoms in the middle of a crystal.
In such a case, the adjacent planes are not straight, but instead bend around the edge of
the terminating plane so that the crystal structure is perfectly ordered on either side.

## Slide 6
Crystal defects
http://www.youtube.com/watch?v=dvDankgGBIs

## Slide 7
Crystal defects
Planar defects
Grain boundaries

## Slide 8
Crystal defects
Planar defects
Twin Boundaries

## Slide 9
Crystal defects
Bulk defects
Voids are small regions where there are no atoms, and can be thought of as clusters of vacancies.
Impurities can cluster together to form small regions of a different phase. These are often called precipitates.

## Slide 10
Macroscopic types of diffusion
Surface diffusion
Grain boundary diffusion
Volume diffusion
Diffusion coefficient of surface diffusion > Diffusion coefficient of grain boundary
diffusion > Diffusion coefficient of volume diffusion

## Slide 12
Mineral B
Mineral B
Mineral A
Mineral B
Mineral A

## Slide 13
Mineral B
Mineral B
Mineral A
Mineral B
Mineral A
Composition of A
Distance (r)
Diffusion to form A
This diffusion is controlled by
the Fick law and it can be
diffusion along the surface or
grain boundary or the volume

## Slide 14
Along the grain
boundries the
diffusion coefficent is
higher than inside the grains
as well at the grain boundries there
is surface energy. The best plase to
start the nucleation is at this place.
In thermdynamic terms: What is the driving force to do that?
Diffusion
It is the chemical potential or to make it simple it is the Gibbs
free energy
G = H − TS

## Slide 15
In thermdynamic terms: What is the driving force to do that?
It is the chemical potential or to make it simple it is the Gibbs
free energy
G = H − TS
dG = dH − T dS
At equilibrium dG = 0
0 = dH − Te dS
dH = Te dS
Where the Te is the
equilibrium temperature
dG = Te dS − T dS
dG = dS (Te − T)
(Te − T) is the super-cooling temperature

## Slide 16
It is not a 2D process but it is 3D process
Where W the work required to grow the mineral, r is the radius
of the mineral and

## Slide 18
r1
r2
r*
W*
To grow a mineral from r1 to r2, you
spend more energy in the surface
than the energy you get from the volume
To grow a mineral you need a nucleus
with radius r*
How can we get r* and W*?

## Slide 19
r1
r2
r*
W*
How can we get r* and W*?

## Slide 20
r1
r2
r*
W*
How can we get r* and W*?
dG = dS (Te − T)
What will happen if we change
the temperature?
If Te = T --- the dG = 0
We need super-cooling to form a new mineral

## Slide 21
r1
r2
r*
W*
Strain term
Where C is composition difference between new mineral and
ground matric, K is bulk moduls and